Production process of the Official Match Ball for the 2010 FIFA World Cup™ in South Africa:

Pre-products:

Pre-products delivered to Longway factory

  - TPU (transparent)

  - EVA 3D panels (white)

  - Bladder including valve (orange)

  - Polyester/cotton fabric (white)

  - Various inks (11 colours), various types of glue

  - Latex compound

A	Carcass – the ball chassis:

- Fabric machining (three steps on one machine)

  - Stretching

  - Fabric lamination with latex

  - Drying

- Automatic cutting of the panels

- Stitching of the carcass

- Metal detection

- Turning carcass

- Weighing of carcass and bladder

- Insert bladder and gluing of the valve

- Carcass shaping

- Spray coating of the latex adhesive onto the carcass

- Drying of the carcass in a hot channel

Carcass ready for final assembling

B	EVA 3D Panels (4 tripods and 4 triangles):

- EVA cutting (triangles and tripods)

- UV-treatment (cleaning process)

- Panel wall cementing

- Top side cementing

EVA ready for the high-frequency vacuum forming with the TPU

C	TPU (delivered as roll):

- TPU sheet cutting (automatic rolling up and cutting)

- Heat-transfer the FIFA World Cup™ logo on TPU

- Flame treatment of the TPU

- TPU printing line

  - Place TPU films onto the print conveyor

  - Underglass printing of 11 different colours

  - Stripping of the printed TPU film (final ball design)

- Cutting and inspection of the 8 different TPU pieces

- TPU films pin hole cutting (CCD hole punching)

- 3D vacuum forming of the TPU films

  - Preparation (apply films on plate)

  - Vacuum forming

  - Detach films

TPU is ready for high-frequency vacuum forming with the EVA

D	High-frequency vacuum bonding of TPU and EVA

- Stock fitting EVA and TPU

- High-frequency vacuum bonding process

- Trimming of the final panels

- Automatic panel cleaning/gluing/drying process

  - Triangle panels	1. cleaning	2. apply glue	  3. drying

  - Tripod panels	1. cleaning	2. apply glue	  3. drying

Panels are ready for assembling

E	Final ball assembling:

- Valve hole punching (valve tripod panel)

- Assemble two ball halves out of 4 panels each

- Weighing two halves (assembled ball panels) and carcass (ideal weight 440 g)

- Centring of the valve on the carcass

- Pre-forming of the carcass and the two ball halves (transparent mould)

- Bonding with air-pressure mould (blue single mould)

- Thermal bonding in heated moulds

- Chilling in cooling tunnel

- Balls rolling out for a final 24 hrs storage / conditioning

Final inspection (weight, circumference, roundness, pressure, visual check of gluing, texture, aero grooves and graphics) and packaging for shipping.